## Slide 1
JINDAL STAINLESS | STAINLESS SPARK | ROUND 2 | PROBLEM STATEMENT 1
Catch every strip defect where it is born, not where it is shipped
AI surface inspection that finds, grades and routes every stainless strip defect to the process that caused it.
52% → 4.7%
clean mill strip wrongly
flagged, before vs after our fix
46% → 90%
of mill-strip defects caught,
before vs after our fix
₹2.5-4.2 cr
per line, vs ₹10-29 cr for a
commercial system
~2.2 years
payback on one line at a
1% downgrade rate
REAL DETECTIONS BY OUR MODEL, ON STEEL IMAGES IT NEVER SAW IN TRAINING
Prathmesh Walimbe · Krishna Kanta Mondal | IIT Bombay
TRY THE LIVE DEMO
surface-vision.github.io
Runs in your browser. Nothing leaves the page.
Photo: Methem, Wikimedia Commons (public domain)
Notes: Cover. The strip of six images is real output from our model on held-out steel images. The QR opens the live demo, which runs in the judge's browser. Four numbers tell the story: on real mill strip we cut false alarms from 52% to 4.7% while roughly doubling the defects caught, at a fraction of commercial cost, paying back in about two years on one line.

## Slide 2
1 Problem
2 Insights
3 Solution
4 Implementation
5 Impact
STAINLESS SPARK ROUND 2 | PS1 | IIT Bombay
A defect born at the caster is paid for at every later stage, but today it is found only at the end
The problem is not that defects exist. They are found late, by sampling, and nobody is told which process caused them.
Sources: AMETEK Surface Vision / Ternium case study (2020); IISE, Measuring the Cost of Quality; ASTM A240; LME nickel USD 16,402/t at INR 95.8/USD (22 Sep 2026); JSL FY26 results.
Where stainless surface defects are born, and where they are seen today
VALUE ADDED KEEPS RISING →
Melt & cast
SMS
Inclusions, slivers
NOT SEEN
Hot rolling
HSM
Scale, pits, edge cracks
NOT SEEN
Anneal & pickle
HRAP
Pickling patches
SPOT CHECK
Cold rolling
CRM
Scratches, roll marks
SPOT CHECK
Final anneal / BA
CRAP / BA
Stains, BA marks
SAMPLED
Finish & despatch
Slit, cut
Found here, or by the customer
CLAIMS
Why it hurts more on stainless
300 m/min
Too fast for the human eye to see the whole surface
₹1.26-1.65 lakh
of nickel in every tonne of 304, given away on a downgrade
2.57 Mt
JSL FY26 sales: each 0.1% downgraded is ~2,570 t
Cost of quality (PAF): where AI inspection moves the money
AI shifts spend from failure (right) to appraisal and prevention (left)
Prevention
Defect sent to its owner in minutes
Appraisal
100% of the surface, one rule for every coil
Internal failure
Caught before more value is added
External failure
Fewer escapes to exposed-finish customers
Cost of poor quality averages ~15% of sales in manufacturing (range 5-35%, IISE).
Notes: Problem. Walk the ribbon left to right: a sliver born at the caster is only seen at finishing, after hot rolling, annealing, pickling and cold rolling have all been paid for. Nickel is why this hurts more on stainless: INR 1.26-1.65 lakh of nickel in every tonne of 304. The cost-of-quality frame is the output: AI inspection is an appraisal cost that moves spend out of internal and external failure. "Seen today" is typical practice; JSL's actual coverage is a P0 input.

## Slide 3
1 Problem
2 Insights
3 Solution
4 Implementation
5 Impact
STAINLESS SPARK ROUND 2 | PS1 | IIT Bombay
On stainless the surface is the product, so every defect type must reach the process that caused it
Classify, don't just alarm: a typed defect becomes a work order for a named owner. The pilot belongs on 300-series cold-rolled strip.
Images: held-out test frames, boxes drawn by our model. Sources: ASSDA; JSL Q1 FY27 results; Leão et al. 2021; Steel in Translation 2023. Owners and grade risks: team hypotheses, to validate with JSL.
Six defect families, six different owners (real detections by our model)
Born: Caster
Owner: SMS
Fix: Tundish level, mould flux
Born: Reheat, hot rolling
Owner: HSM
Fix: Reheat and coiling temperature
Born: Hot rolling
Owner: HSM
Fix: Descaler pressure, nozzles
Born: Reheat, pickling
Owner: HSM / pickling
Fix: Furnace atmosphere, over-pickling
Born: Anneal & pickle
Owner: Pickling line
Fix: Acid strength, line speed
Born: Cold rolling, handling
Owner: CRM / logistics
Fix: Guides, rolls, coil handling
Three facts that change the brief
The finish cannot be repaired. 2B/BA damage cannot be polished out (ASSDA).
Surface-critical tonnes are growing. Cold rolling 2.05 → 2.67 MTPA by FY28.
End markets see the surface. Auto, rail, metros, white goods (Q1 FY27).
Grade-by-defect risk: which defects to train for first
Grade | Slivers | Scale | Scratches | Edge cracks | Ridging
200 series (Cr-Mn) | M | M | H | M | L
300 series (304, 316) | H | M | H | L | L
400 series (409, 430) | H | M | M | M | H
Duplex (2205) | M | H | M | H | L
OUTPUT 300 series is the pilot grade: highest exposed-finish risk and the most nickel per tonne.
Notes: Insights, stainless-specific. The six images are our model's real detections on held-out frames. Each family is born at a different stage, so a typed detection can go straight to the right owner as a work order. The owner mapping draws on the metallurgy literature and needs a JSL metallurgist's sign-off in P0. The grade matrix is a hypothesis; its output is the pilot grade, 300 series.

## Slide 4
1 Problem
2 Insights
3 Solution
4 Implementation
5 Impact
STAINLESS SPARK ROUND 2 | PS1 | IIT Bombay
Our tests produced four findings, and each one changed the design
The model is the cheap part. JSL's own strip, the image resolution and trustworthy confidence decide whether the system works.
All numbers measured by us on three public steel-surface datasets, on images the model never saw in training.
1 A model that never saw clean steel cries wolf
Chart: 
| Clean strip wrongly flagged | Defects caught
Trained on lab images only | 51.7 | 46.2
With real clean strip added (ours) | 4.7 | 89.6
So we: train on JSL's own clean and defective strip before any alarm is trusted.
2 A bigger model or sharper images did not help
Compact model
0.752
baseline
+ clean strip (ours)
0.764
no extra cost
Model 3.7x larger
0.734
3.5x compute
4x sharper images
0.734
4x pixels
All four compared at the same image size; bars start at 0.70. The shipped model runs larger, trading 0.02 here for +0.11 on real mill strip.
So we: keep the model compact and spend the budget on camera coverage.
3 Line speed, not the model, sets the hardware bill
~18 processors
see every 0.2 mm of a 1.28 m strip at 250 m/min
vs
1 processor
if images are coarsened to 1.28 mm, but fine scratches vanish
So we: fix the image resolution with JSL first, then size the hardware.
4 Operators act only on alarms they can trust
60% lower
confidence error after calibration, so a stated confidence is now within about 3 points of how often it is actually right
0 of 3,200
real steel images wrongly rejected by our "is this steel?" check, which stops the system judging anything else
So we: every alarm carries a trustworthy confidence and a steel check.
Notes: Four findings from our own tests, each of which changed the design. One: a model trained only on lab defect images flags 155 of 300 clean mill images; adding real clean strip cuts that to 14 and nearly doubles the real defects it catches. Two: a bigger model and sharper images did not improve accuracy, so money goes into cameras. Three: at full detail a 250 m/min line needs about 18 processors; resolution is a spec decision we make with JSL on day one. Four: operators act only on alarms they trust, so every alarm carries a calibrated confidence and passes an is-this-steel check.

## Slide 5
1 Problem
2 Insights
3 Solution
4 Implementation
5 Impact
STAINLESS SPARK ROUND 2 | PS1 | IIT Bombay
Detect on the strip, decide at the coil, route to the owner, and learn from every correction
Buy proven cameras, own the model: vendor-grade capture with a detector trained on JSL's grades and wired to JSL's process owners.
BUILT = working in our prototype today, live at surface-vision.github.io. Unlabelled-learning result: J. Mater. Inf. 2025. Commercial price range: industry figure, unverified.
How it works: six stages from camera to corrective action
Capture
Cameras on both faces, down to 0.2 mm
TO BUILD
Check
Is it usable steel? If not, skip it
BUILT
Detect
Find and classify every defect
BUILT
Score
Confidence, severity 0-100, coil position
BUILT
Decide
Accept, downgrade or hold, per grade
PARTIAL
Act & learn
Alert, hold, work order; corrections retrain it
TO BUILD
Running today
Upload a strip image, get: • box on the defect
• defect type
• confidence
• severity score
surface-vision.github.io runs in the browser
What is new beyond a standard detector
Trained on clean strip too
false alarms 52% → 4.7%
Root-cause routing
every alarm becomes a work order
Unseen-defect check
flags patterns never labelled (proposed)
Learns from unlabelled coils
JSL's image archive becomes an asset
Build vs buy
Cost per line
Proven at speed
Tuned to JSL grades
JSL owns model
Commercial
USD 1-3M (unverified)
Fully in-house
₹2-3 cr (est.)
Hybrid (ours)
₹2.5-4.2 cr (est.)
strong
partial
weak
Output: hybrid is never weak.
Notes: Solution. Stages 2 to 4 are built and running today, including in the browser demo. Stage 5 has coil rules built, but grade- and finish-specific limits need JSL input. Stages 1 and 6 are the plant-side pilot work. What makes this more than a standard detector: it is trained on clean strip as well as defects, every defect is routed to the process that caused it, a second check catches defects it was never taught, and it can learn from JSL's unlabelled image archive. Build vs buy: commercial systems are proven but cost USD 1-3M per line and keep the model closed; hybrid is never weak.

## Slide 6
1 Problem
2 Insights
3 Solution
4 Implementation
5 Impact
STAINLESS SPARK ROUND 2 | PS1 | IIT Bombay
It already works on public steel data; the pilot's job is to prove it on JSL's own strip
Strong on four of six defect families today. Every weak spot is known, and each has a fix in the pilot plan.
Datasets: NEU-DET (Northeastern Univ.); Severstal steel defects (Kaggle); GC10-DET (Lv et al. 2020, CC BY 4.0). All scores on held-out images the model never saw in training; model chosen on validation across four training runs.
Tested on three public steel datasets
NEU-DET
1,800 images, 6 defect types
University benchmark, hot-rolled strip
Severstal
12,568 real mill frames
Production strip from a steel mill
GC10-DET
2,294 frames, 10 types
Full-width line-scan camera frames (roll marks shown)
How well it finds each defect type (accuracy, held-out images)
published range
Patches
0.94
Inclusion
0.80
Scratches
0.79
Pitted surface
0.76
Rolled-in scale
0.60
Crazing
0.58
Headline results
178 of 180
test images: the right defect type named
~55 ms
per image, running in an ordinary laptop browser
~10,100
images across three datasets, for training and testing
Known weak spots, and the fix for each
Weak spot | Today (0-1) | Fix in the pilot
Low-contrast texture: crazing, rolled-in scale | 0.58-0.60 | Angled lighting; JSL labels in P1
Real mill frames are harder than the lab benchmark | 0.57 vs 0.75 | Train on JSL's own strip in P1
Roll marks and edge cracks: few examples | 0.20 | Edge cameras; targeted labelling
Notes: Proof. Three public datasets, about 10,100 images, all scored on images the model never saw in training. Per defect, four of six families sit at or above the published range; crazing and rolled-in scale are low-contrast textures and are weaker. The honest headline is the second weak spot: on real mill frames accuracy is 0.57 against 0.75 on the lab benchmark. That is exactly why P1 trains on JSL's own strip before anything is trusted. Roll marks score 0.20 on GC10 because there are only a few dozen examples; edge cameras and targeted labelling fix that.

## Slide 7
1 Problem
2 Insights
3 Solution
4 Implementation
5 Impact
STAINLESS SPARK ROUND 2 | PS1 | IIT Bombay
Seven months to shadow mode on one line, and nothing touches the mill until trust is earned
Commit ₹2.5-4.2 cr and one line for seven months. The month-7 go/no-go is decided on JSL's own alarm and recall numbers.
Costs are team estimates for a 1.3-1.6 m line inspected on both faces, at INR 95.8/USD, to be replaced by vendor quotes in P0. KPI targets to be agreed with JSL Quality in P0.
Stage-gate roadmap (months)
m0
m4
m8
m12
m16
m20
EXIT GATE
P0
Instrument one line
Resolution and grade matrix fixed
P1
Train on JSL strip
Clean alarms ≤ 25%, recall ≥ 90%
P2
Shadow mode: advises only
≥ 90% operator agreement
P3
Auto-hold on severe defects
Holds trusted; downgrade measured
P4
Second line and grade
Fleet decision on real payback
pilot go / no-go
Cost per line, estimated
Chart: 
| Cameras & lighting | Installation & integration | Computing hardware | Training on JSL strip
Cost | 115 | 120 | 60 | 40
₹2.5-4.2
cr per line
Cameras & lighting
₹85-145 L
Installation & integration
₹90-150 L
Computing hardware
₹45-75 L
Training on JSL strip
₹30-50 L
Running cost ~₹50 L a year
Top risks, and when each is retired
Risk | Mitigation | Retired
Model does not transfer to JSL strip | Train on JSL clean and defect images | P1
Low-contrast defects missed | Angled lighting, sharper images | P0-P1
Rare defects under-learnt | Edge cameras, targeted labelling | P1-P3
Operators ignore alarms | Trusted scores, shadow mode first | P2
Heat, dust, acid fumes | Sealed, cooled enclosures | P0
Pilot KPIs: how JSL will know it works
≥ 90%
defective strip flagged
measured 258 of 288 (89.6%)
≤ 25%
clean strip wrongly flagged
measured 4.7% on mill strip
≤ 5 pts
confidence vs reality gap
measured 3.3 pts
< 0.2 s
defect to operator screen
design target
≥ 90%
operator agreement, shadow
measured in P2
< 8 h
retrain for a new grade
measured 0.6 h
Notes: Implementation. Five phases, 20 months, with a hard go/no-go at month 7 after shadow mode. The system never acts on the mill until P3; before that it only reads data and advises. Cost is our estimate, INR 2.5-4.2 crore per line, against USD 1-3M (about INR 10-29 crore) for a commercial system; vendor quotes replace it in P0. Two of the six pilot targets are already met on public mill strip and a third is within half a point; P1 exists to prove the same on JSL's own strip, which no public dataset can answer.

## Slide 8
1 Problem
2 Insights
3 Solution
4 Implementation
5 Impact
STAINLESS SPARK ROUND 2 | PS1 | IIT Bombay
At a conservative 1% downgrade rate one line pays back in ~2.2 years; the fleet protects ~₹13 cr a year
Recommendation: approve a 7-month pilot on one 300-series cold-rolled line. JSL's own downgrade rate decides fleet rollout.
Inputs: JSL FY26 (INR 1,67,407/t; 25,65,902 t). Base: 0.4 Mt line, 30% of loss recovered, ₹3.35 cr capex, ₹0.5 cr/yr run cost, 12% rate. Commercial: USD 2M at INR 95.8.
Loss pool per line, ₹ cr a year
0.4 Mt × downgrade rate × price discount × ₹1,67,407/t
Downgraded | 10% off | 15% off | 20% off
0.5% of volume | 3.3 | 5.0 | 6.7
1.0% of volume | 6.7 | 10.0 | 13.4
2.0% of volume | 13.4 | 20.1 | 26.8
Base case (dark): ₹6.7 cr pool. Recover 30% = ₹2.0 cr/yr, ₹1.5 cr net of run cost. Fleet (2.57 Mt): ₹43 cr pool, ₹12.9 cr/yr recovered.
Payback per line, base case
Hybrid (ours)
2.2 yr
Commercial system
12.7 yr
+₹2.1 cr 5-year NPV per line at 12%
≥ 0.11% of line revenue lost to downgrade is enough for a 2-year payback
What moves payback (years)
Downgrade rate 0.5-2%
0.9-6.6
Share recovered 15-45%
1.3-6.6
Line volume 0.3-0.5 Mt
1.7-3.3
Capex ₹2.5-4.2 cr
1.7-2.8
Price discount 10-20%
0.9-2.2
base 2.2 yr
Impact beyond the P&L
Coverage
100% of both faces, every coil
Customers
Defect map per coil, fewer claims
Process
Defects tied to heat and coil IDs
Safety
Severe-defect holds prevent strip breaks
Sustainability
Less remelt, acid and nickel waste
People
Inspectors move to decisions
WHAT WE ASK OF JSL
One 300-series cold-rolled line, 7 months
₹2.5-4.2 cr pilot budget
Downgrade rate by line and grade
A metallurgist at 20% for root causes
In return: measured downgrade rate, payback and a go / no-go at month 7.
Notes: Impact. At 1% of volume downgraded at a 10% discount, one 0.4 Mt line loses INR 6.7 crore a year; recovering 30% less INR 0.5 crore run cost pays back INR 3.35 crore capex in about 2.2 years, against 12.7 years for a commercial system. Downgrade rate and recovery share dominate the tornado; neither is public, so both are measured in P2-P3 before fleet spend. Close on the ask.