## Slide 1: Catch every strip defect at the line, not at the customer
JINDAL STAINLESS | CASE COMPETITION | PROBLEM STATEMENT 1
EXECUTIVE SUMMARY
AI-POWERED SURFACE DEFECT DETECTION
A 6.22 MB computer-vision model that detects, classifies and scores surface defects in real time, calibrated to what a wrong call costs the mill, and running live today.
TEAM
Futuristic
Krishna Kanta Mondal · Prathmesh Walimbe
IIT Bombay
TRY THE LIVE DEMO
surface-vision.github.io
The trained detector, running in your browser. Upload a strip image; nothing leaves the page.
Six defect families shown on held-out test frames.
Slide 1: problem and solution. Slide 2: validation, roadmap and value.
Notes: Cover. Team details are placeholders to fill in before submission. The QR code opens https://surface-vision.github.io, the shipped detector running client-side.

## Slide 2: Why is late detection costly, and what did we build to fix it?
1 Problem
2 Solution
3 Validation
4 Roadmap and value
JINDAL STAINLESS | PS1 | Futuristic
PROBLEM AND SOLUTION
1 / 2
Cost of Late Detection
research_notes s2a, s4a
inclusions
Casting
scale, crazing, edge cracks
Hot rolling
pits, patches
Anneal, pickle
roll marks, scratches
Cold rolling
scratches
Finishing
Customer
AI target: classify each defect where it is born
Found today: by eye, or by the customer
8-10%
nickel in grade 304 by mass, so a stainless downgrade costs more
300 m/min
strip speed at which the human eye cannot inspect the full surface
~15%
of sales lost to poor quality in manufacturing, range 5-35%
Model Options Tested
model_study, gap1 reports
OPTION
mAP50
COST
VERDICT
YOLOv8n at 256 px
0.752
3.0 M params
CHOSEN
YOLOv8n + Severstal clean strip
0.764
same size
READY
YOLOv8s, 3.7x the parameters
0.734
3.5x FLOPs
NO GAIN
YOLOv8n retrained at 640 px
0.734
4x pixels
NO GAIN
Test-time augmentation
-0.006
2.39x latency
REJECTED
Held-out test, scored once. Nano vs small: 95% CI [-0.008, +0.042] spans zero.
Solution Architecture
src/inference.py, src/report.py
1 Capture
4 cameras across a 1.28 m strip at 0.2 mm/px
TO BUILD
2 Tile
64 tiles per frame, so full resolution survives
BUILT
3 Detect
YOLOv8n, 6.22 MB; threshold 0.15 set by a cost model
BUILT
4 Decide
severity 0-100; coil ACCEPT, DOWNGRADE or HOLD
BUILT
5 Act
HMI alert, PLC hold, MES record with root cause
TO BUILD
EVERY DEFECT RETURNS
Bounding box
Defect type
Calibrated confidence
Severity 0-100
Root cause and fix
Closed loop (proposed): operator overrides feed active learning; a per-line retrain takes 0.6 h.
Live Demo
checked 13 Sep 2026
surface-vision.github.io
Upload a strip image
Box, type, confidence, severity
30-50 ms per frame on CPU
No image leaves the browser
Late, sampled inspection is the cost. A 6 MB detector that classifies every defect at line speed and names its process owner is the fix, and it already runs live.
Notes: Problem: defects are born upstream (inclusions at the caster, scale and crazing at hot rolling) but found at finishing or by the customer, after every process step has been paid for. Sources: nickel share of 304 and the IISE cost-of-quality range from docs/research_notes.md s4a; 300 m/min from the AMETEK/Ternium case study, s2a. Options: reports/model_study.json (nano vs small bootstrap, TTA), resolution_study (640 px retrain), gap1_detection_metrics.json (joint model 0.7642). Architecture: tiling, detection and the coil decision are built; cameras and PLC/MES are not.

## Slide 3: Does it meet the brief, and what should Jindal do first?
1 Problem
2 Solution
3 Validation
4 Roadmap and value
JINDAL STAINLESS | PS1 | Futuristic
PROOF AND ROLLOUT
2 / 2
Scorecard Against the Brief
reports/*.json, exec_summary_checks.json
CONSIDERATION
EVIDENCE, HELD-OUT DATA
STATUS
NEXT STEP
Detection accuracy
mAP50 0.752 on held-out test; all 180 defective frames flagged
MET
-
False-alarm rate
Clean strip flagged 93.7% -> 32.5% after joint training; confidence calibrated, ECE 0.142 -> 0.046
PARTIAL
Jindal clean strip, P1
Multiple defect types
Type right on 177/180 frames. AP50: scratches 0.91, scale 0.63, roll marks 0.20; no public edge-crack data
PARTIAL
Plant labelling, P1
Line-speed inference
6.22 MB, 30-50 ms per frame on CPU. At 250 m/min: 18 accelerators at 0.2 mm/px, or 1 downscaled
MET
Resolution spec, P0
Usable demo
Live web demo: upload an image, get box, type, confidence, severity and root cause
MET
-
Scaling across grades
Second dataset: cross-domain AUC 0.608 -> 0.958 and in-domain mAP50 up to 0.764; retrain 0.6 h
PARTIAL
Stainless grades, P1-P4
Training on Real Clean Strip
gap1 reports, conf 0.15
Shipped, NEU-DET only
Joint, + Severstal
Clean strip flagged, %
lower is better
32.5
93.7
Defect recall, %
72.0
86.6
Cross-domain AUC x100
60.8
95.8
In-domain mAP50 x100
75.2
76.4
0
50
100
473 of 505 clean Severstal frames flagged before, 164 after
Pilot Roadmap, 20 Months
phase plan; 0.6 h retrain measured
PHASE
EXIT GATE
m0
m4
m8
m12
m16
m20
P0 Instrument one line
Frames captured at line speed
P1 Fine-tune on Jindal strip
Clean-strip alarms under target
P2 Shadow mode, no interlock
Operator-verified alarm rate
P3 PLC hold on severe defects
Hold decisions trusted
P4 Second line and grade
Fleet rollout decision
pilot go / no-go
Business Case
research_notes s3a, FY26
2.57 Mt x 1% downgraded x 10% discount x INR 167,407/t
= INR 43 cr a year at risk
Downgraded \ discount
10%
15%
20%
0.5% of volume
21
32
43
1.0% of volume
43
64
86
2.0% of volume
86
129
172
Recovering 30% is about INR 13 cr a year: payback 0.7-2 years on a USD 1-3M line system (unverified range).
Needed from Jindal: the real downgrade rate.
Recommendation: approve a 7-month pilot on one line, ending in shadow mode. The model already clears accuracy, speed and demo; only Jindal's own strip can close false alarms, roll marks and edge cracks.
Notes: Scorecard sources: reports/model_study.json (mAP50 0.7524), gap1_cross_domain.json (473/505 clean frames flagged before, 164/505 after; defect crop recall 72.0% to 86.6%; AUC 0.608 to 0.958), calibration.json (ECE), gc10_coverage.json (roll marks 0.203), evaluation at 256 px (scratches 0.909, rolled-in scale 0.630), benchmark.json mill.scenarios at 250 m/min and 320 px (18 accelerators tiled, 1 downscaled), deck/build/exec_summary_checks.json (177/180 type correct and 180/180 flagged at conf 0.15). Business case: FY26 volume and realisation are Jindal reported figures; the downgrade rate and discount are swept, not known; the system cost is an unverified USD 1-3M industry range, so payback is quoted as a range.